SCHEDULE ‘D’

| TECHNICAL DATA SCHEDULE 330 kV TRANSMISSION LINE ACSR 350 mm2 CONDUCTOR CODE NO: 4601 |
| --- |
| ITEM | DESCRIPTION | UNITS | REQUIRED | GUARANTEED |
| 1.0 | Manufacturer | - | - | China National Electric Wire&Cable Corp. |
| 1.1 | Type | - | ACSR | ACSR |
| 1.2 | Code Name |  | BISON | BISON |
| 1.3 | Details of material and standard to which conforming Steel Aluminium Zinc Composite conductor |  |  | Steel Aluminium Zinc Composite conductor |
| 1.4 | Designation | - | - |  |
| 1.5 | Country of Origin | - | - | China |
| 2.0 | Mechanical characteristics and dimensions |  |  |  |
| 2.1 | Stranding | - | 54/7 | 54/7 |
| 2.2 | Aluminium wire diameter | mm | 3.0 | 3.0 |
| 2.3 | Galvanized steel wire diameter | mm | 3.0 | 3.0 |
| 2.4 | Overall diameter | mm | 27 | 27 |
| 2.5 | Aluminium area | mm2 | 381.7 | 381.7 |
| 2.6 | Steel area | mm2 | 49.5 | 49.5 |
| 2.7 | Nominal Aluminium area | mm2 | 350 | 350 |
| 2.8 | Greased | - | Yes (drop point 120C) | Yes (drop point 120C) |
| 2.9 | Mass | kg/km | 1443 | 1443 |
| 2.10 | Rated tensile strength | kN | 120.9 | 120.9 |
| 2.11 | Initial lower modulus of elasticity | Gpa | - |  |
| 2.12 | Initial upper modulus of elasticity | Gpa | - |  |
| 2.13 | Transition stress | Mpa | - |  |
| 2.14 | Final modulus of elasticity | Gpa | - |  |
| 2.15 | Equivalent temperature difference for Creep compensation | 0C | - |  |
| 2.16 | Coefficient of linear thermal expansion | E-6/0C | - |  |
| 2.17 | D.c. resistance at 200C | ohms/km | 0.07573 | 0.07573 |
| 2.18 | Lay ratio( Max. and min.) Steel core 6 layer Aluminium 12layer 18 layer 24 layer |  |  | Steel core 6 layer Aluminium 12layer 18 layer 24 layer |
| 2.19 | Weight Aluminium wire Before stranding After stranding Galvanized steel wire Before stranding After stranding | Kg/km |  | 1055.3 349.5 |
| 3.0 | Transport |  |  |  |
| 3.1 | Standard length of conductor per reel | m | - | 2500 |
| 3.2 | Maximum number of standard lengths per reel |  | 1 |  |
| 3.3 | Flange diameter | mm | - |  |
| 3.4 | Inside traverse | mm | - | 1100 |
| 3.5 | Overall width | mm | - | 1400 |
| 3.6 | Drum diameter | mm | - | 2000 |
| 3.7 | Minimum cover from edge of flange | mm | 25 | 50 |
| 3.8 | Arbor hole diameter | - | - |  |
| 3.9 | Material | mm | Seasoned soft Wood | Steel-wood |
| 3.10 | Empty reel mass | kg | - | 410 |
| 3.11 | Thickness of lagging | mm | - | 0 |
| 3.12 | Shipping mass | kg |  | 4017.5 |
| 3.13 | Shipping volume | m3 | - | 4.396 |
| 3.14 | Max. back tension the drum is suitable to with stand from the tensioner used for tension stringing | N |  |  |
| 3.15 | Drum drawing indicating dimensions , bill of material, marking, end fixation arrangement, etc. |  |  |  |
| 4.0 | Standards |  |  |  |
| 4.1 | Manufacturing | - | IEC 61089 BS 215 IEC 61394 IEC 60889 | IEC 61089 BS 215 IEC 61394 IEC 60889 |
| 4.2 | Quality Assurance | - | ISO 9001 | ISO 9001 |
| 5.0 | Installation |  | Outdoor Desertic/ Tropical environment | Outdoor Desertic/ Tropical environment |

General Notes

- Tolerances, where applicable, may be indicated

- No joint shall be made in the aluminium strand of the outer layer of the conductor.

- No joint is permitted in the steel core

- The parameters of aluminium and steel strands and their chemical composition may also be furnished and guaranteed.

| TECHNICAL DATA SCHEDULE 132 kV TRANSMISSION LINE ACSR 250 mm2 CONDUCTOR CODE NO: 4602 |
| --- |
| ITEM | DESCRIPTION | UNITS | REQUIRED | GUARANTEED |
| 1.0 | Manufacturer | - | - | China National Electric Wire&Cable Corp. |
| 1.1 | Type | - | ACSR | ACSR |
| 1.2 | Code Name |  | BEAR | BEAR |
| 1.3 | Details of material and standard to which conforming Steel Aluminium Zinc Composite conductor |  |  | Steel Aluminium Zinc Composite conductor |
| 1.4 | Designation | - | - |  |
| 1.5 | Country of Origin | - | - | China |
| 2.0 | Mechanical characteristics and dimensions |  |  |  |
| 2.1 | Stranding | - | 30/7 | 30/7 |
| 2.2 | Aluminium wire diameter | mm | 3.35 | 3.35 |
| 2.3 | Galvanized steel wire diameter | mm | 3.35 | 3.35 |
| 2.4 | Overall diameter | mm2 | 23.45 | 23.45 |
| 2.5 | Aluminium area | mm2 | 264.4 | 264.4 |
| 2.6 | Steel area | mm2 | 61.7 | 61.7 |
| 2.7 | Nominal Aluminium area | mm2 | 250 | 250 |
| 2.8 | Greased | - | Yes (drop point 120C) | Yes (drop point 120C) |
| 2.9 | Mass | kg/km | 1214 | 1214 |
| 2.10 | Rated tensile strength | kN | 111.2 | 111.2 |
| 2.11 | Initial lower modulus of elasticity | GPa | - |  |
| 2.12 | Initial upper modulus of elasticity | GPa | - |  |
| 2.13 | Transition stress | MPa | - |  |
| 2.14 | Final modulus of elasticity | GPa | - |  |
| 2.15 | Equivalent temperature difference for Creep compensation | 0C | - |  |
| 2.16 | Coefficient of linear thermal expansion | E-6/0C | - |  |
| 2.17 | Lay ratio( Max. and min.) Steel core 6 layer Aluminium 12layer 18 layer |  |  | Steel core 6 layer Aluminium 12layer 18 layer |
| 2.18 | Weight Aluminium wire Before stranding After stranding Galvanized steel wire Before stranding After stranding | Kg/km |  | 730.7 483.5 |
| 2.19 | D.C. resistance at 200C | ohms/km | 0.1093 | 0.1093 |
| 3.0 | Transport |  |  |  |
| 3.1 | Standard length of conductor per reel | m | - |  |
| 3.2 | Maximum number of standard lengths per reel |  | 2 |  |
| 3.3 | Flange diameter | mm | - |  |
| 3.4 | Inside traverse | mm | - | 1100 |
| 3.5 | Overall width | mm | - | 1400 |
| 3.6 | Drum diameter | mm | - | 2000 |
| 3.7 | Minimum cover from edge of flange | mm | 25 | 50 |
| 3.8 | Arbor hole diameter | - | - |  |
| 3.9 | Material | mm | Wood | Steel-wood |
| 3.10 | Empty reel mass | kg | - | 409 |
| 3.11 | Thickness of lagging | mm | - | 0 |
| 3.12 | Shipping mass | kg | 1500 max. | 4293.8 |
| 3.13 | Shipping volume | m3 | - | 4.396 |
| 3.14 | Max. back tension the drum is suitable to with stand from the tensioner used for tension stringing |  |  |  |
| 3.15 | Drum drawing indicating dimensions , bill of material, marking, end fixation arrangement, etc. |  |  |  |
| 4.0 | Standards |  |  |  |
| 4.1 | Manufacturing | - | IEC 61089 BS 215 IEC 61394 IEC 60889 | IEC 61089 BS 215 IEC 61394 IEC 60889 |
| 4.2 | Quality Assurance | - | ISO 9001 | ISO 9001 |
| 5.0 | Installation |  | Outdoor Desertic/ Tropical environment | Outdoor Desertic/ Tropical environment |

Notes

- Tolerances, where applicable, may be indicated

- No joint shall be made in the aluminium strand of the outer layer of the conductor.

- No joint is permitted in the steel core

- The parameters of aluminium and steel strands and their chemical composition may also be furnished and guaranteed.

- Where two lengths of conductor are in one drum, a red tag will be placed at a distance of 50m from the finishing end of each length and a temporary weld joint be made to inform the stringing supervisor about the finish end of one conductor length.

| TECHNICAL DATA SCHEDULE OVERHEAD GALVANIZED STEEL GROUND WIRE CODE NO: 4701 |
| --- |
| ITEM | DESCRIPTION | UNITS | REQUIRED | GUARANTEED |
| 1.0 | Manufacturer | - | - | China National Electric Wire&Cable Corp. |
| 1.1 | Type | - | Zinc-coated steel wire strand | Zinc-coated steel wire strand |
| 1.2 | Designation |  | - |  |
| 1.3 | Details of material and standard to which conforming Steel Zinc Composite Ground wire |  |  | Steel Zinc Composite Ground wire |
| 1.3 | Country of Origin | - | - | China |
| 2.0 | Mechanical characteristics and dimensions |  |  |  |
| 2.1 | Number of wires | - | 7 | 7 |
| 2.2 | Wire diameter | mm | 3.25 | 3.25 |
| 2.3 | Overall diameter | mm | 9.8 | 9.8 |
| 2.4 | Steel area | mm2 | 58.1 | 58.1 |
| 2.5 | Mass | kg/km | 460 | 460 |
| 2.6 | Steel grade | - | Extra-high strength | Extra-high strength |
| 2.7 | Elongation (sample 200mm) | - | - | - |
| 2.8 | Ultimate tensile strength | kN | 66.8 | 66.8 |
| 2.9 | Modulus of elasticity | h Bar | 1800 | 1800 |
| 2.10 | Equivalent temperature difference for Creep compensation | 0C |  |  |
| 2.11 | Zinc coating class and weight of zinc coating | g/m2 | - |  |
| 2.12 | D.C.resistance | Ohm/km | - |  |
| 2.13 | Lay length | mm | - |  |
| 2.14 | Details of protective coating given on ground wire to prevent formation of white rust during shipment and storage |  |  |  |
| 3.0 | Transport |  |  |  |
| 3.1 | Standard length of conductor per reel | m | - | 3000 |
| 3.2 | Maximum number of standard lengths per reel |  | 1 | 3000 |
| 3.3 | Flange diameter | mm | - |  |
| 3.4 | Inside traverse | mm | - |  |
| 3.5 | Overall width | mm | - | 700 |
| 3.6 | Drum diameter | mm | - | 1100 |
| 3.7 | Minimum cover from edge of flange | mm | 25 | 50 |
| 3.8 | Arbor hole diameter | - | - |  |
| 3.9 | Material | mm | Seasoned soft Wood | Steel-wood |
| 3.10 | Empty reel mass | kg | - | 105 |
| 3.11 | Thickness of lagging | mm | - | 0 |
| 3.12 | Shipping mass | kg | - | 1485 |
| 3.13 | Shipping volume | m3 | - | 0.664 |
| 3.14 | Max. back tension the drum is suitable to with stand from the tensioner used for tension stringing |  |  |  |
| 3.15 | Dimensionded Drum drawing, BoM, marking, end fixation arrangement, etc. |  |  |  |
| 4.0 | Standards |  |  |  |
| 4.1 | Manufacturing | - | BS 183 IEC 60888 | BS 183 IEC 60888 |
| 4.2 | Quality assurance | - | ISO 9001 | ISO 9001 |
| 5.0 | Installation |  | Outdoor Desertic/ Tropical environment | Outdoor Desertic/ Tropical environment |

Notes

- Tolerances, where applicable, may be indicated

- No joint is permitted in the steel wire

- The parameters of steel strands and their chemical composition may also be furnished and guaranteed.